Supplementary Information

Reactive template synthesis of Li1.2Mn0.54Ni0.13Co0.13O2 nanorod cathode for Li-ion batteries: Influence of temperature over structural and electrochemical properties

Murugan Vivekananthaa,b, Chenrayan Senthila, Thangaian Kesavana, Thamodaran Partheebana, Mani Navaneethanb, Baskar Senthilkumarc, Prabeer Barpandad, and Manickam Sasidharana*

aSRM Research Institute and Department of Chemistry, SRM Institute of Science and Technology, Kattankulathur, Chennai, 603 203, India

bDepartment of Physics and Nanotechnology, SRM Institute of Science and Technology, Kattankulathur, Chennai, 603 203, India

cLaboratoire de Réactivité et de Chimie des Solides (LRCS), CNRS UMR 7314, Université de Picardie Jules Verne, 80039 Amiens Cedex, France

dFaraday Materials Laboratory, Materials Research Center, Indian Institute of Science, Bangalore 560012, India

Fig. S1. XRD of β-MnO2

Fig. S1 shows the XRD pattern of β-MnO2 , all the peaks were matched with the JCPDS card no 81-2261

Fig. S2. Raman spectra of LLO-15

Fig. S2 shows the Raman spectra for LLO-15, the strong peaks at 615 cm-1 and 495 cm-1 is derived to the A1g and Eg symmetric stretching modes of R-3m space group and the peaks around 565 cm-1 and 450cm-1 corresponds to Ag and Bg modes of Li2MnO3 belonging to the C 2/m space group. These results confirm the presence of both the phases in LLO-15 [1].

Fig. S3. Raman spectra of LLO-15

Fig. S3 gives the FTIR spectra for LLO-15. The peak observed around 597 cm-1 corresponds to the asymmetric stretching vibrations of MO6 and the peak at 545cm-1 corresponds to the bending vibrations of O – M –O bonds [2].

Fig. S4. BET surface analysis of LLO-15

BET surface analysis was done to check the surface area and porosity of the LLI-15 sample and is shown in Fig. S4. From the analysis it was found that the sample had a surface area of             30.67 m2 g-1 with a pore volume 0.036 cc cm-1. Fig. S4 inset shows the average pore size for the sample.

Fig. S5. (a & b) CV curves of LLO-9 and LLO-12 samples and (c) cycle number vs discharge capacity plots LLO-9 and LLO-12

Fig. S6. (a-c) EIS before and after cycling at different temperatures (d) EIS of cell before and after cycling

Fig. S7. Plots of real part of impedance as a function of inverse square root of angular frequency

Table S1 Crystallographic parameters of Li1.2Mn0.54Ni0.13Co0.13O2 dwelled at different time

Table S2 Structural parameters obtained from Rietveld refinement of XRD data for LLO-15

| S. No. | Morphology | Current Density/ C Rate | Capacity (mAh/g) | Reference |
| --- | --- | --- | --- | --- |
| 1. | Nanotubes | 5C | 118 | [3] |
| 2. | Flakes | 5C | 80 | [4] |
| 3. | Micro particles | 1250 mA /g | 104 | [5] |
| 4. | Nanoflakes | 5C | 118 | [6] |
| 5. | Nanoparticles | 4C | 120 | [7] |
| 6. | Micro particles | 5C | 100 | [8] |
| 7. | Na+ and (PO4) 3- doped nanoparticles | 5C | 132 | [9] |
| 8. | Nanoplates | 5C | 113 | [10] |
| 9. | Hierarchical Microspheres | 5C | 102 | [11] |
| 10 | Nanorods | 5C | 130 | This Work |

Table S3. Comparison of present results with literature data

Table S4 Impedance and diffusion values for the cell cycled at 1C at 25, 55 and 5 ºC

(Circuit shown in Fig 5f inset)

References

| [1] R.E. Ruther, A.F. Callender, H. Zhou, S.K. Martha, J. Nanda, Raman microscopy of lithium-manganese-rich transition metal oxide cathodes, J. Electrochem. Soc. 162 (2015) A98–A102. doi:10.1149/2.0361501jes. [2] P. Manikandan, P. Periasamy, Novel mixed hydroxy-carbonate precursor assisted synthetic technique for LiNi1/3Mn1/3Co1/3O2 cathode materials, Mater. Res. Bull. 50 (2014) 132–140. doi:10.1016/j.materresbull.2013.10.010. [3] D. Ma, Y. Li, M. Wu, L. Deng, X. Ren, P. Zhang, Enhanced cycling stability of Li-rich nanotube cathodes by 3D graphene hierarchical architectures for Li-ion batteries, Acta Mater. 112 (2016) 11–19. doi:10.1016/j.actamat.2016.04.010. [4] Y.-C. Jin, J.-G. Duh, Hierarchically-structured nanocrystalline lithium rich layered composites with enhanced rate performances for lithium ion battery, Energy Storage Mater. 6 (2017) 157–163. doi:10.1016/j.ensm.2016.10.009. [5] Y. Zhou, Y. Wang, S. Li, J. Mei, H. Liu, H. Liu, G. Liu, Irregular micro-sized Li1.2Mn0.54Ni0.13Co0.13O2 particles as cathode material with a high volumetric capacity for Li-ion batteries, J. Alloys Compd. 695 (2017) 2951–2958. doi:10.1016/j.jallcom.2016.11.375. [6] L. Ma, Y. Li, Z. Chen, F. Zhang, P. Ding, L. Mao, F. Lian, Improved rate capability of Li-rich cathode materials by building a Li+ conductive LixBPO4+ x/2 Nanolayer from residual Li2CO3 on the surface, ChemElectroChem. 4 (2017) 1443–1449. doi:10.1002/celc.201700157. [7] P. K. Nayak, J. Grinblat, E. Levi, T.R. Penki, M. Levi, Y.-K. Sun, B. Markovsky, D. Aurbach, Remarkably improved electrochemical performance of Li- and Mn-rich cathodes upon substitution of Mn with Ni, ACS Appl. Mater. Interfaces. 9 (2017) 4309–4319. doi:10.1021/acsami.6b07959. [8] J.-L. Shi, D.-D. Xiao, M. Ge, X. Yu, Y. Chu, X. Huang, X.-D. Zhang, Y.-X. Yin, X.-Q. Yang, Y.-G. Guo, L. Gu, L.-J. Wan, High-capacity cathode material with high voltage for Li-ion batteries, Adv. Mater. 30 (2018) 1705575. doi:10.1002/adma.201705575. [9] Y. Liu, D. Ning, L. Zheng, Q. Zhang, L. Gu, R. Gao, J. Zhang, A. Franz, G. Schumacher, X. Liu, Improving the electrochemical performances of Li-rich Li1.20Ni0.13Co0.13Mn0.54O2 through a cooperative doping of Na+ and (PO4)3− with Na3PO4, J. Power Sources. 375 (2018) 1–10. doi:10.1016/j.jpowsour.2017.11.042. [10] J. Li, T. Jia, K. Liu, J. Zhao, J. Chen, C. Cao, Facile design and synthesis of Li-rich nanoplates cathodes with habit-tuned crystal for lithium ion batteries, J. Power Sources. 333 (2016) 37–42. doi:10.1016/j.jpowsour.2016.09.150. [11] M. Lou, H. Zhong, H.-T. Yu, S.-S. Fan, Y. Xie, T.-F. Yi, Li1.20Ni0.13Co0.13Mn0.54O2 hollow hierarchical microspheres with enhanced electrochemical performances as cathode material for lithium-ion battery application, Electrochim. Acta. 237 (2017) 217–226. doi:10.1016/j.electacta.2017.03.201. |  |
| --- | --- |