Supporting Information

Structural and Electrochemical Investigation of Binary Na2Fe1-xZnxP2O7    (0 ≤ x ≤ 1) Pyrophosphate Cathodes for Sodium-ion Batteries

Ritambhara Gond,‡ Sher Singh Meena,§ Valerie Pralong† and Prabeer Barpanda‡*

‡ Faraday Materials Laboratory, Materials Research Center,

Indian Institute of Science, C.V. Raman Avenue, Bangalore, 560012, India.

§ Solid State Physics Division, Bhabha Atomic Research Center, Bombay, 400014, India.

†Normandie Univ, ENSICAEN, UNICAEN, CNRS, CRISMAT, Caen, 14000, France.

* authors for correspondence

E-mail: prabeer@iisc.ac.in

Phone: +91-80 2293 2783; Fax: +91-80 2360 7316

Table S1 Crystallographic data, lattice parameters and atomic coordinates of Na2FeP2O7 and Na2ZnP2O7 compound derived from Rietveld refinement of high resolution X-ray diffractogram (λ= 1.5404 Å) data collected at 300 K.

Na2FeP2O7

| Formula Weight Crystal System Space group Unit cell parameter (Å) Unit cell volume (Å3) Theoretical Density (g cm-3) Fitness parameters (R values) | Na2FeP2O7 [275.7 g mol-1] Monoclinic P-1 (#2) a = 6.43596(16), b = 9.44757(22), c = 11.04744(25) α = 64.2(49)º β = 85.3(70)º γ= 72.9(29)º, Z = 4 577.51 3.17 Rp = 1.34, Rwp = 2.02 , R(f2) = 7.6 |  |
| --- | --- | --- |
| Atoms | x | Y | Z | Occ. | Uiso(Å2) | Wyckoff position |
| Fe1 | 0.721(4) | 0.393(2) | 0.216(9) | 1 | 0.0001(3) | 2i |
| Fe2 | 0.645(1) | -0.001(7) | 0. 265(5) | 1 | 0.0001(2) | 2i |
| P1 | 0. 575(8) | 0. 205(0) | 0.458(3) | 1 | 0.0001(8) | 2i |
| P2 | 0.122(9) | 0.048(1) | 0.313(8) | 1 | 0.0001(8) | 2i |
| P3 | 0.074(5) | 0.325(7) | 0.788(5) | 1 | 0.0001(8) | 2i |
| P4 | 0.289(5) | 0.690(0) | 0.037(4) | 1 | 0.0001(8) | 2i |
| Na1 | 0.028(3) | 0.316(2) | 0.474(8) | 1 | 0.0003(6) | 2i |
| Na2 | 0.410(7) | 0.642(8) | 0.338(1) | 1 | 0.0003(6) | 2i |
| Na3 | 0.211(6) | 0.346(4) | 0.103(1) | 1 | 0.0003(6) | 2i |
| Na4 | 0.500(0) | 0.0 | 0.0 | 0.33333 | 0.0003(6) | 1d |
| Na5 | 0.189(9) | 0.007(6) | 0.043(2) | 0.5 | 0.0003(6) | 2i |
| Na6 | 0.377(8) | 0.01(8) | 0.017(1) | 0.33333 | 0.0003(6) | 2i |
| O1 | 0.016(9) | 0.221(7) | 0.302(1) | 1 | 0.0001(3) | 2i |
| O2 | 0.653(6) | 0.354(8) | 0.434(5) | 1 | 0.0001(3) | 2i |
| O3 | 0.303(7) | 0.036(4) | 0.221(2) | 1 | 0.0001(3) | 2i |
| O4 | 0.113(2) | 0.439(2) | 0.846(0) | 1 | 0.0001(3) | 2i |
| O5 | 0.767(6) | 0.045(2) | 0.538(1) | 1 | 0.0001(3) | 2i |
| O6 | 0.284(5) | 0.180(1) | 0.809(5) | 1 | 0.0001(3) | 2i |
| O7 | 0.029(1) | 0.040(6) | 0.695(9) | 1 | 0.0001(3) | 2i |
| O8 | 0.771(6) | 0.397(3) | 0.036(6) | 1 | 0.0001(3) | 2i |
| O9 | 0.427(8) | 0.573(8) | 0.169(4) | 1 | 0.0001(3) | 2i |
| O10 | 0.619(8) | 0.177(2) | 0.051(2) | 1 | 0.0001(3) | 2i |
| O11 | 0.373(8) | 0.196(5) | 0.535(8) | 1 | 0.0001(3) | 2i |
| O12 | 0.554(3) | 0.201(7) | 0.324(3) | 1 | 0.0001(3) | 2i |
| O13 | 0.087(1) | 0.768(7) | 0.102(3) | 1 | 0.0001(3) | 2i |
| O14 | 0.03(9) | 0.604(2) | 0.344(1) | 1 | 0.0001(3) | 2i |

Na2ZnP2O7

| Formula Weight Crystal System Space group Unit cell parameter (Å) Unit cell volume (Å3) Theoretical Density (g cm-3) Fitness parameters (R values) | Na2ZnP2O7 [285.31 g mol-1] Tetragonal P42/n (#86) a = b = 21.78065(35), c = 10.29645(20) α = β = γ= 90º, Z = 32 4884.60(1) 3.10 Rp = 6.29, Rwp = 9.86, R(f2) = 8.78 |
| --- | --- |
| Atoms | x | Y | Z | Occ. | Uiso(Å2) | Wykoff position |
| Zn1 | 0.250(0) | 0.250(0) | 0.250(0) | 1 | 0.0003(2) | 2a |
| Zn2 | 0.750(0) | 0.750(0) | 0.250(0) | 1 | 0.0003(3) | 2b |
| Zn3 | 0.750(0) | 0.250(0) | 0.246(6) | 1 | 0.0003(1) | 4e |
| Zn4 | 0.507(4) | 0.503(9) | 0.250(0) | 1 | 0.0003(2) | 8g |
| Zn5 | 0.494(4) | 0.748(6) | 0.250(9) | 1 | 0.0003(1) | 8g |
| Zn6 | 0.253(4) | 0.494(9) | 0.249(9) | 1 | 0.0003(2) | 8g |
| Na1 | 0.446(0) | 0.622(9) | 0.000(2) | 1 | 0.0003(3) | 8g |
| Na2 | 0.473(3) | 0.627(0) | 0.493(0) | 1 | 0.0003(0) | 8g |
| Na3 | 0.383(7) | 0.275(3) | 0.007(8) | 1 | 0.0002(3) | 8g |
| Na4 | 0.374(3) | 0.304(4) | 0.499(5) | 1 | 0.0003(0) | 8g |
| Na5 | 0.695(8) | 0.374(1) | 0.000(4) | 1 | 0.0003(4) | 8g |
| Na6 | 0.724(3) | 0.368(9) | 0.490(6) | 1 | 0.0003(7) | 8g |
| Na7 | 0.379(2) | 0.444(0) | 0.498(7) | 1 | 0.0002(8) | 8g |
| Na8 | 0.628(0) | 0.526(3) | 0.006(3) | 1 | 0.0002(7) | 8g |
| P1 | 0.697(9) | 0.621(3) | 0.216(3) | 1 | 0.0001(7) | 8g |
| P2 | 0.560(8) | 0.628(8) | 0.207(5) | 1 | 0.0002(0) | 8g |
| P3 | 0.627(2) | 0.438(8) | 0.289(4) | 1 | 0.0002(1) | 8g |
| P4 | 0.621(2) | 0.302(2) | 0.283(6) | 1 | 0.0001(9) | 8g |
| P5 | 0.370(4) | 0.688(2) | 0.292(7) | 1 | 0.0001(3) | 8g |
| P6 | 0.378(5) | 0.552(2) | 0.287(7) | 1 | 0.0001(7) | 8g |
| P7 | 0.447(5) | 0.377(8) | 0.213(1) | 1 | 0.0001(7) | 8g |
| P8 | 0.311(4) | 0.370(8) | 0.211(3) | 1 | 0.0001(4) | 8g |
| O1 | 0.713(9) | 0.559(9) | 0.148(4) | 1 | 0.0002(5) | 8g |
| O2 | 0.738(0) | 0.670(9) | 0.162(4) | 1 | 0.0002(9) | 8g |
| O3 | 0.694(1) | 0.619(5) | 0.360(1) | 1 | 0.0002(5) | 8g |
| O4 | 0.630(2) | 0.64(3) | 0.157(5) | 1 | 0.0002(1) | 8g |
| O5 | 0.527(5) | 0.683(4) | 0.140(9) | 1 | 0.0001(9) | 8g |
| O6 | 0.542(3) | 0.568(9) | 0.146(8) | 1 | 0.0002(1) | 8g |
| O7 | 0.559(9) | 0.626(9) | 0.354(0) | 1 | 0.0002(5) | 8g |
| O9 | 0.627(3) | 0.439(3) | 0.142(1) | 1 | 0.0002(7) | 8g |
| O10 | 0.580(2) | 0.479(6) | 0.351(8) | 1 | 0.0002(3) | 8g |
| O11 | 0.689(7) | 0.450(5) | 0.357(5) | 1 | 0.0002(9) | 8g |
| O12 | 0.607(0) | 0.371(5) | 0.34(1) | 1 | 0.0001(9) | 8g |
| O13 | 0.623(9) | 0.304(2) | 0.141(6) | 1 | 0.0002(3) | 8g |
| O14 | 0.682(7) | 0.286(1) | 0.347(3) | 1 | 0.0002(3) | 8g |
| O15 | 0.569(3) | 0.265(1) | 0.347(8) | 1 | 0.0001(9) | 8g |
| O16 | 0.367(2) | 0.688(9) | 0.146(6) | 1 | 0.0002(1) | 8g |
| O17 | 0.317(7) | 0.720(9) | 0.357(1) | 1 | 0.0002(7) | 8g |
| O18 | 0.430(9) | 0.709(9) | 0.357(6) | 1 | 0.0002(1) | 8g |
| O19 | 0.358(7) | 0.618(4) | 0.342(5) | 1 | 0.0002(4) | 8g |
| O20 | 0.382(9) | 0.553(1) | 0.141(3) | 1 | 0.0002(5) | 8g |
| O21 | 0.328(1) | 0.510(5) | 0.345(4) | 1 | 0.0002(3) | 8g |
| O22 | 0.440(0) | 0.537(7) | 0.350(7) | 1 | 0.0002(0) | 8g |
| O23 | 0.469(9) | 0.318(8) | 0.147(2) | 1 | 0.0003(2) | 8g |
| O24 | 0.482(6) | 0.430(7) | 0.152(8) | 1 | 0.0002(4) | 8g |
| O25 | 0.446(9) | 0.379(0) | 0.360(0) | 1 | 0.0002(4) | 8g |
| O26 | 0.379(8) | 0.385(7) | 0.156(4) | 1 | 0.0002(3) | 8g |
| O27 | 0.271(9) | 0.422(0) | 0.144(6) | 1 | 0.0002(0) | 8g |
| O28 | 0.298(8) | 0.309(7) | 0.150(4) | 1 | 0.0002(4) | 8g |
| O29 | 0.311(1) | 0.368(3) | 0.353(4) | 1 | 0.0001(5) | 8g |

Figure S1. Tetragonal crystal structure showing eight crystallographic sites of Na in the single unit cell.

Figure S2 Comparative powder X-ray diffraction patterns of solid-state synthesized binary Na2(Fe1-xZnx)P2O7 (0 ≤ x ≤ 1) compounds. Increase in Zn content leads to a phase transition from monoclinic crystal (P-1) to tetragonal crystal (P42/n) system as observed in solution combustion synthesis.

Figure S3. Charge-discharge capacity plot for the Na2FeP2O7 (red) and Na2(Fe0.75Zn0.25)P2O7 (blue) samples at C/20 rate in 2.0-4.0 V. The initial 5 cycles are shown for the comparison.

Figure S4. Typical charge-discharge profile of Na2ZnP2O7 (P42/n) prepared by combustion method revealing Zn as redox inactive species with its microstructure (inset SEM image).

Figure S5. QOCP curves of combustion synthesized Na2FeP2O7 (left) and Na2Fe0.75Zn0.25P2O7 (right) measured at C/50 showing thermodynamic potential of ~2.9 V and ~3.1 V respectively.