Cyanogenic Glycosides: A Sustainable Carbon and Nitrogen Source for Developing Resilient Janus Reversible Oxygen Electrocatalysts for Metal-air Batteries

Ravi Nandana,b,* and Sankalpa Nanda c

aMaterials Research Centre,

Indian Institute of Science,

Bangalore -560012, India.

Ph. No. +91-080-2293 2996. Fax: +91-80-2360 7316.

* Email:-  aerawat27@gmail.com; ravinandan@iisc.ac.in ; ravinand@jaist.ac.jp (Dr. Ravi Nandan, ORCID 0000-0001-9244-3594)

b(Present address) Japan Advanced Institute of Science and Technology,

1-Ashaidai, Nomi City, Ishikawa 923-1211,

Japan.

cChrist (Deemed to be university), Bangalore-560029, India

Fig. S1 Schematic representation of ANi700/ANi8500/ANi1000 synthesis arrangement.

Fig. S2 (a,b) Raman spectra recorded on ANi700 and ANi1000.

Fig. S3 Deconvoluted HRXPS spectra of (a) C1s, (b) N1s and (c) Ni2p for ANi700.

Fig. S4 Deconvoluted HRXPS spectra of (a) C1s, (b) N1s and (c) Ni2p for ANi1000.

Fig. S5 TEM, HRTEM, Fourier transform of selected area as indicated by yellow box and corresponding inverse Fourier transform for interplanar spacing evaluation for (a-d) ANi700 and (e-g) ANi1000. The estimated planar spacing suggests the presence of (111) and (200) NiO planes in nanoparticles randomly selected from ANi700 and ANi1000, respectively.

Fig. S6 Cyclic voltammograms in non-Faradic region for Cdl determination (Figure 4c) in nitrogen-purged 0.1 M NaOH aqueous solution at different potential scan speed of (10-100 mV/s) recorded on (a) ANi700, (b) ANi850 and (c) ANi1000, respectively.

Fig. S7 Electrochemical impedance study using Nyquist plots on ANi700, ANi850 and ANi1000 in 0.1 M NaOH aqueous solution at 0.965 V vs RHE.

Fig. S8 Accelerated stability test on ANi850 using RDE-LSV setup (50th, 500nd and 3000nd cycles of ORR polarization curves in alkaline (0.1 M NaOH) medium at rotation speed of 1400 rpm and 100 mV/s scan speed).

Table S1. ORR activity summary for various recently developed transition metal based carbon nanocomposites in alkaline medium.

Fig. S9 RDE-LSV OER polarization curves (50th and 3000nd cycles) on ANi850 for accelerated stability test in nitrogen purged alkaline (1 M NaOH) aqueous solution at 1200 rpm and 100 mV/s scan speed.

Table S2. OER activity summary for various transition metal based carbon nanocomposites  in alkaline medium.

| Electrocatalyst | Electrocatalyst loading | Eon-set (V) Vs RHE | EJ=10 (V) Vs RHE | Reference |
| --- | --- | --- | --- | --- |
| CoFe2O4/rGO | 1.006 mg/cm2 | ~ 1.504 | ~ 1.664 | Journal of Power Sources 250 (2014) 196-203 |
| FeCo2O4-HrGOS | 1.006 mg/cm2 | ~ 1.534 | ~ 1.714 | Carbon 92 ( 2015) 74 –83 |
| CoFe2O4/CNTs | 1.006 mg/cm2 | ~ 1.564 | ~ 1.664 | Electrochimica Acta 177 (2015) 65–72 |
| MWCNT@S–N–C | 0.200 mg/cm2 | ~ 1.564 | ~ 1.664 | New J. Chem., 2015, 39, 6289--6296 |
| S,N,Fe-porous carbon | 0.100 mg/cm2 | ---- | ~ 1.614 | Green Chem., 2016, 18, 4004-4011 |
| N-doped Fe-Fe3C@ graphitic layer | 0.710 mg/cm2 | ~ 1.564 | ~ 1.742 | Green Chemistry 18 (2016), 427-432 |
| Nitrogen-doped Fe/Fe3C@graphitic layer/carbon nanotube | 0.103 mg/cm2 | ~ 1.464 | ~ 1.814 | Chem. Commun., 2015, 51, 2710-2713 |
| NiCo2S4@N/SrGO | 0.283 mg/cm2 | ~ 1.564 | ~ 1.684 | ACS Appl. Mater. Interfaces, 2013, 5 (11), pp 5002–5008 |
| Fe3C-NCNTs co-embedded boron doped carbon | 0.75 mg/cm2 | ~ 1.445 | ~ 1.585 | J. Mater. Chem. A, 2017, 5, 16843-16853 |
| Fe3C-FeNx enriched carbon sphere | 1 mg/cm2 | ~ 1.403 | ~ 1.573 | J. Mater. Chem. A, 2018, 6, 8537 |
| FeNi encapsulated NCNTs (FN10R) | 0.4 mg/cm2 | ~ 1.488 | ~ 1.568 | J. Mater. Chem. A, 2018, 6, 20411-20420 |
| Ni Co2.7(OH)x | 0.2 mg/cm2 | ~ 1.48 | ~ 1.62 | Adv. Energy Mater., 2015, 5, 1401880. |
| ANi850 | 0.1 mg/cm2 | ~ 1.5 (@ 2 mA/cm2) | ~ 1.55 | Present study |

Table S3. Overall oxygen electroactivity (E) summary for various carbon-based electrocatalysts in alkaline medium.

| Catalyst | Overall oxygen electrochemistry ΔE (Ej=10(OER) – E1/2(ORR)) (V) | Reference |
| --- | --- | --- |
| S-N-C@MWNCNTs | ~1.25 | New J. Chem. 2015, 39, 6289. |
| Co3O4/2.7Co2MnO4 | ~ 1.17 V | Nanoscale, 2013, 5, 5312–5315 |
| Ni/N-CTs | ~ 1.09 V | J. Mater. Chem. A,2016, 4, 1694–1701 |
| NCNF-1000 | ~1.02 | Adv. Mater. 2016, 28, 3000−3006. |
| Fe/Fe3C@NGL-NCNT | ~1 | Chem. Commun. 2015, 51, 2710. |
| N-Graphene/CNTs | ~1.00 | Small, 2014, 10, 2251. |
| B-MWNCNTs | ~1.00 | Electrochimica Acta 2014,143, 291. |
| CoFe2O4/rGO | ~0.98 | J. Power Sources 2014, 250, 196. |
| CoFe2O4/N-P-biocarbon | ~0.98 | J. Mater. Chem. A 2014,2,18012. |
| N,P-Carbon paper | ~ 0.96 | Angew. Chem. Int. Ed. 2015, 54, 4646. |
| P-doped g-C3N4 /CF | ~0.96 | Angew. Chem. Int. Ed. 2015, 54, 4646−4650. |
| Fe/Fe3C@ N-graphitic layer | ~ 0.97 | Green Chem., 2016, 18, 427–432 |
| NGM-Co | 0.95 V | Adv. Mater. 2017, 29, 1703185 |
| Pt@C | ~0.94 | Angew. Chem. Int. Ed. 2014, 53, 8508. |
| MnxOy/N-Carbon | ~0.93 | Angew. Chem. Int. Ed. 2014, 53, 8508. |
| Ir@C | ~0.92 | J. Am. Chem. Soc. 2010,132, 3612. |
| NiCo2O4/Graphene | ~0.915 | J. Mater. Chem. A 2013,1,4754. |
| N, S, O carbon nanosheet | ~0.88 | Nano Energy 19 (2016) 373–381 |
| Fe@N-C | ~0.88 | Nano Energy 2015, 13, 387−396. |
| ANi850 | ~0.845 | Present study |

# Text boxes

(a)

(b)

| Electrocatalyst | Electrocatalyst loading | Eon-set (V) Vs RHE | E1/2 Vs RHE | Reference |
| --- | --- | --- | --- | --- |
| MWCNT@S–N–C | mg/cm2 | ~0.764 | ~0.614 | New J. Chem., 2015, 39, 6289--6296 |
| CoFe2O4/CNTs | 1.006 mg/cm2 | ~0.840 | ~0.664 | Electrochimica Acta 177 (2015) 65–72 |
| CoFe2O4/rGO | 1.006 mg/cm2 | ~0.828 | ~0.704 | Journal of Power Sources 250 (2014) 196e203 |
| Co–N–GN | 0.1 mg/cm2 | ~0.866 | ~0.802 | J. Mater. Chem. A, 2013, 1, 3593-3599 |
| N,P,S-rGO/E. coli | 0.510 mg/cm2 | ~0.874 | ~0.764 | J. Mater. Chem. A 2015,3, 12873-12879 |
| FeCo2O4-HrGOS | 1.006 mg/cm2 | ~0.874 | ~0.764 | Carbon 92 (2015 74-83 |
| N-graphene/CNT hybrids | 0.430 mg/cm2 | ~0.884 | ~0.764 | Angew. Chem. Int. Ed. 2014, 53, 6496 - 6500 |
| N-CNTs | 0.306 mg/cm2 | ~0.904 | ~0.744 | Carbon 50 (2012) 2620-2627 |
| N,S-Graphene | 0.43 mg/cm2 | ~0.904 | ~0.664 | Angew. Chem., Int. Ed., 2012, 51, 11496 |
| Fe3C-NCNTs co-embedded boron doped carbon | 0.75 mg/cm2 | ~0.934 | ~0.739 | J. Mater. Chem. A, 2017, 5, 16843-16853 |
| N-doped Fe-Fe3C@ graphitic layer | 0.71 mg/cm2 | ~0.914 | ~0.739 | Green Chem., 2016, 18, 427–432 |
| FeNi encapsulated NCNTs (FN10R) | 0.4 mg/cm2 | ~0.899 | ~0.700 | J. Mater. Chem. A, 2018, 6, 20411-20420 |
| ANi850 | 0.1 mg/cm2 | ~0.950 (@ 0.05 mA/cm2) | ~0.705 | Present study |