Supplementary Materials for

Nanoforest of 3C-SiC/graphene by laser chemical vapor deposition with high electrochemical performance

Qingyun SUN1, Rong TU1, Qingfang XU1, Jun LI2, Hitoshi OHMORI3, Marina KOSINOVA4, Bikramjit BASU5, Jiasheng YAN6, Shusen LI6, Song ZHANG1,*, Takashi GOTO1, Lianmeng ZHANG1

1 State Key Laboratory of Advanced Technology for Materials Synthesis and

Processing, Wuhan University of Technology, 122 Luoshi Road, Wuhan 430070, China

2 National Key Laboratory for Shock Wave and Detonation Physics, Institute of Fluid

Physics, P.O. Box 919-102, Minyan, 621900, China

3 Institute of Physical and Chemical Research, 2-1 Hirosawa, Wako, Saitama

351-0198, Japan

4 Nikolaev Institute of Inorganic Chemistry, Russian Academy of Sciences Siberian

Branch, 3 Acad. Lavrerntiev Pr. Novosibirsk, 630090, Russia

5 Centre for BioSystems Science and Engineering, Indian Institute of Science, Bangalore 560012, Karnataka, India

6 Tech Semiconductors, LTD., No.162 Shengli Street, Xiangyan, 441021, China

*Corresponding author, Song ZHANG: Tel/Fax: +86-27-87499409;

E-mail: kobe@whut.edu.cn

Fig. S1. Effects of Tdep and Ptot on the morphologies of films prepared by LCVD.

Fig. S2. TEM observations of the pyramid-like 3C-SiC films deposited at Tdep = 1623 K and Ptot = 400 Pa.

Fig. S3. Wettability of the films with different morphologies deposited at different Tdep and Ptot. (A): Nanoforest-like films deposited at Tdep = 1523 K and Ptot = 400 Pa. (B): Flower-like films deposited at Tdep = 1573 K and Ptot = 800 Pa. (C): Pyramid-like films deposited at Tdep = 1623 K and Ptot = 400 Pa.