Supporting Information

Dual Role of N-Doped Carbon Dots Dispersed Transparent Polymer Film: A High-Efficiency Blue Light Converter and UV Screener

Barun Kumar Barman1, 2, Tadaaki Nagao1, 3 * and Karuna Kar Nanda1, 2 *

1International Center for Materials Nanoarchitectonics (MANA), National Institute for Materials Science (NIMS), Tsukuba, Ibaraki 305-0044, Japan

2Materials Research Centre, Indian Institute of Science, Bangalore-560012, India

3Department of Condensed Matter Physics Graduate School of Science, Hokkaido University, Kita-10 Nishi-8 Kita-ku, Sapporo 060-0810, Japan

*Correspondence should be addressed to NAGAO.Tadaaki@nims.go.jp, nanda@iisc.ac.in

Fig. S1 Excitation-dependent fluorescence spectra of N-CDs in PVA solution.

Fig. S2 (a and b) Fitted TRPL spectra of N-CD/PVA solid film and solution.

The lifetime of N-CDs in solution and solid was fitted using a bi-exponential function Y(t) based on non‐linear least squares analysis in Equation;1, 2

Y(t) = A1exp(-t/) + A2exp(-t/)

Where A1 and A2 are the fractional contributions of time‐resolved decay lifetimes of τ1 and τ2.

The average lifetime of the quantum dots (avg) was calculated using the following equation;

avg = (A1A2 A1 + A2

|  | A1 |  | A2 |  | avg |
| --- | --- | --- | --- | --- | --- |
| N-CD solid film | 1.931 | 1.594 | 0.7488 | 4.908 | 10.72 |
| N-CD solution | 10.01 | 0.84 | 0.523 | 4.24 | 1.54 |

Fig. S3 The PL spectrum of N-CD/PVA film, which is stable in atmospheric conditions for several days without any change in PL properties.

Table S1: Blue luminescent carbon/grapheme quantum dots

| Materials | Precursors | Solvent | Method | Ex dep/Indep | Emi (nm) | QY soln | QY Solid | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| N, S-CDs | 3-cyclopentylpropionic acid and EDA and NaOH | water | Hydro | Indep | 472 | 54.4 | ------ | Nanoscale, 2014, 6, 13817 |
| N-CQDs | ammonium citrate and ethylenediamine | water | Hydro |  | 445 | 66.8 | ------- | J. Mater. Chem. C, 2015, 3, 1922 |
| N-CDs | citric acid and ethylenediamine | water | Hydro | Dep | 443 | 80 | ------ | Angew. Chem. Int. Ed. 2013, 52, 1-6 |
| N-CDs | citric acid and ethylenediamine | water | Hydro |  | 445 | 37 |  | ACS Appl. Mater. Interfaces 2018, 10, 29902-29908 |
| N-CDs | citric acid monohydrate ethylenediamine | water | Hydro |  | 445 |  | 45 (CD/PVP) | Nanoscale, 2015, 7, 12045 |
| N-CQDs | isophorone diisocyanate |  | Microwave | dep | 440 | 11 |  | Nanoscale, 2016, 8, 4742 |
| N-CDs/LDH | citric acid monohydrate ethylenediamine | Water | Hydro |  | 440 |  | 61.63 | J. Mater. Chem. C, 2017, 5, 3536 |
| N-CDs/CTAB | citric acid and urea | DMF | Solvo | dep |  |  | PVP-CDs White light 38.7 | J. Mater. Chem. C, 2017, 5, 11416 |
| N-Dots | 2-azidoimidazole | MeOH | Normal heat | dep |  | 14 |  | Angew. Chem. Int. Ed. 2014, 53, 12542 –12547 |
| NCD | PVA and EDA | water | Hydro | dep | 414 |  | 36 | Adv. Mater. 2016, 28, 312–318 |
| CNDs | oleylamine and different MW of polyacrylamide | water | Normal heat | dep |  | 40 | ------ | Chem. Mater. 2013, 25, 1893-1899 |
| C-Dots | CA and Urea | water | Microwave | dep | 420 | 14 | 40 (Lens paper) | Angew. Chem. Int. Ed. 2012, 51, 12215 –12218 |
| Si-CDs gel | Organosilane + citric acid | water | Heating |  | 435 | 47 | 88 (in gels) | Adv. Mater. 2012, 24, 1716–1721 |
| CDs | CA + Urea | water | microwave |  | 500 | 17 | 61 (CDs/PVA) | Scientific rep, 2016, 6, 19991 |
| GQDs | citric acid monohydrate ethylenediamine | water | hydro | Indep | 450 | 94 | --------- | Sci. Rep. 4, 5294; DOI:10.1038/srep05294 (2014) |
| Functionalized N-CDs/PVA | C powder and nitric acid and EDA | water |  |  | 480 |  | 32 (PVA matrix) | J. Mater. Chem. C, 2016, 4, 6967-6974 |
| CDs | citric acid and urea | Water | microwave |  | 515 |  | 50 (starch) | Nanoscale, 2014, 6, 13076 |
| CDs | thiosalicylic acid and ethylenediamine | water | hydrothermal |  | 475 | 51.4 |  | Appl. Phys. Lett. 2015, 107, 213102. |
| CDs | Citric acid+ EDA | water | hydrothermal |  | 470 | 60 | 45 (PVP matrix) | Nanoscale, 2015, 7, 12045–12050 |
| N-doped hydroxyl functionalized CDS | tris(hydroxylmethyl)aminomethane + EDA | water | Microwave |  | 410 | 99 |  | Nanoscale, 2016, 8, 15281–15287 |
| N,S-Co-doped Carbon dots | Citric acid + L-cysteine | Water | hydrothermal | Indep | 420 | 78 | 60 (polyhedral oligomeric silsesquioxane(POSS) matrix) | : Chem. Commun., 2015, 51, 2950 |
| N-CDs | CA + EDA + trace amount of HCl | Water | hydrothermal | Indep | 440 | 80 | 91 (PVA matrix) | Our Work |

Reference

- H. Zhong, Y. Zhou, M. Ye, Y. He, J. Ye, C. He, C. Yang, Y. Li, Controlled Synthesis and Optical Properties of Colloidal Ternary Chalcogenid CuInS2 Nanocrystals, Chem. Mater 20 (2008) 6434- 6443.

- Y. Deng, D. Zhao, X. Chen, F. Wang, H. Songa, D. Shen, Long lifetime pure organic phosphorescence based on water soluble carbon dots, Chem. Commun 49 (2013) 49, 5751-5753.