SUPPORTING INFORMATION

High responsivity and photovoltaic effect based on vertical transport in multi-layer α-In2Se3

Roop K. Mech*, Neha Mohta, Avijit Chatterjee, Shankar Kumar Selvaraja, Rangarajan Muralidharan and Digbijoy N. Nath

Centre for Nano Science and Engineering (CeNSE), Indian Institute of Science, Bengaluru, Karnataka

Corresponding author, email: roopmech@iisc.ac.in

S1. Transient Performance of the Vertical α-In2Se3 Photodetector

Figure S1. Transient performance of the vertical α-In2Se3 photodetector on a fresh sample and after 2 weeks storage showing excellent performance and stability.

S2. Photocurrent response of the Vertical α-In2Se3 Photodetector

Figure S2. Photocurrent measurement on the vertical α-In2Se3 photodetector for a fresh sample and after 2 weeks storage showing ITO can be an excellent encapsulation layer for In2Se3 photodetector.