Fig S1: Nodules from siliceous ooze sediment showing varied texture, shape and size. The scale of dimension is in centimeter.

Fig S1: Continues….

Fig S2: Nodules from siliceous (SS-3/139 to SS-4/217A) and siliceous-red clay transition zone sediment (SS-3/187 to AAS-40/325). The scale of dimension is in centimeter.

Fig S3: Nodules from siliceous-red clay transition zone (SS-4/225A) and red clay sediment (SS-8/541B to SS-4/237B). The scale of dimension is in centimeter.

Table S1: Electron microprobe analysis of the microlayers of selected nodule samples from core to rim; all values are in wt%.

| Sample | Host sediment | Genetic type | DataSet/Point | Mn | Fe | Co | Ni | Cu | Mn/Fe | Ni+Cu+Co |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 262 | Sili-Red clay | Mixed | 1 | 37.24 | 5.76 | 0.03 | 0.62 | 1.55 | 6.47 | 2.20 |
|  |  |  | 2 | 32.97 | 4.26 | 0.08 | 0.79 | 1.53 | 7.74 | 2.41 |
|  |  |  | 3 | 37.69 | 3.02 | 0.03 | 1.10 | 2.07 | 12.47 | 3.19 |
|  |  |  | 4 | 37.51 | 0.75 | 0.06 | 0.83 | 2.01 | 50.26 | 2.90 |
|  |  |  | 5 | 41.96 | 0.09 | - | 0.57 | 2.56 | 449.84 | 3.14 |
|  |  |  | 6 | 34.68 | 1.06 | 0.01 | 1.09 | 2.01 | 32.81 | 3.11 |
|  |  |  | 7 | 39.02 | 0.58 | 0.00 | 0.85 | 1.96 | 66.94 | 2.81 |
|  |  |  | 8 | 0.32 | 11.05 | - | 0.01 | 0.13 | 0.03 | 0.14 |
|  |  |  | 9 | 8.24 | 15.66 | 0.05 | 0.09 | 0.39 | 0.53 | 0.53 |
|  |  |  | 10 | 0.49 | 15.77 | - | 0.02 | 0.26 | 0.03 | 0.28 |
|  |  |  | 11 | 9.49 | 11.20 | 0.01 | 0.24 | 0.55 | 0.85 | 0.80 |
|  |  |  | 12 | 25.46 | 5.15 | 0.03 | 0.71 | 1.33 | 4.95 | 2.07 |
|  |  |  | 13 | 0.19 | 10.04 | - | 0.05 | 0.10 | 0.02 | 0.15 |
|  |  |  | 14 | 0.29 | 9.00 | 0.00 | 0.01 | 0.22 | 0.03 | 0.22 |
|  |  |  | 15 | 21.12 | 4.24 | 0.03 | 0.52 | 1.14 | 4.98 | 1.70 |
|  |  |  | 16 | 29.15 | 2.47 | 0.06 | 0.65 | 1.75 | 11.79 | 2.46 |
|  |  |  | 17 | 0.53 | 3.53 | 0.00 | 0.03 | 0.14 | 0.15 | 0.16 |
|  |  |  | 18 | 0.36 | 7.38 | 0.00 | 0.01 | 0.10 | 0.05 | 0.10 |
| 291 | Siliceous | Mixed | 1 | 0.03 | 0.37 | 0.00 | 0.01 | - | 0.08 | 0.01 |
|  |  |  | 2 | 0.01 | 0.40 | 0.01 | 0.00 | 0.01 | 0.02 | 0.02 |
|  |  |  | 3 | 0.05 | 0.34 | 0.01 | - | 0.02 | 0.14 | 0.02 |
|  |  |  | 4 | 0.05 | 0.40 | - | - | - | 0.12 | - |
|  |  |  | 5 | 0.01 | 0.33 | - | 0.00 | - | 0.02 | 0.00 |
|  |  |  | 6 | 0.07 | 0.34 | 0.00 | 0.00 | - | 0.20 | 0.00 |
|  |  |  | 7 | 32.86 | 4.38 | 0.06 | 0.89 | 2.73 | 7.51 | 3.68 |
|  |  |  | 8 | 19.07 | 10.38 | 0.08 | 0.23 | 0.57 | 1.84 | 0.88 |
|  |  |  | 9 | 21.00 | 7.48 | 0.03 | 0.37 | 0.88 | 2.81 | 1.28 |

| Sample | Host sediment | Genetic type | DataSet/Point | Mn | Fe | Co | Ni | Cu | Mn/Fe | Ni+Cu+Co |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 10 | 23.33 | 8.27 | 0.03 | 0.45 | 0.95 | 2.82 | 1.43 |
|  |  |  | 11 | 28.25 | 9.52 | 0.09 | 0.44 | 0.84 | 2.97 | 1.36 |
|  |  |  | 12 | 26.49 | 9.34 | 0.07 | 0.49 | 1.27 | 2.84 | 1.83 |
|  |  |  | 13 | 23.73 | 8.85 | 0.04 | 0.38 | 0.75 | 2.68 | 1.18 |
|  |  |  | 14 | 11.90 | 5.29 | 0.05 | 0.16 | 0.34 | 2.25 | 0.54 |
|  |  |  | 15 | 27.14 | 10.27 | 0.12 | 0.38 | 0.88 | 2.64 | 1.37 |
|  |  |  | 16 | 21.13 | 8.07 | 0.07 | 0.45 | 1.02 | 2.62 | 1.54 |
|  |  |  | 17 | 27.05 | 9.18 | 0.06 | 0.41 | 0.86 | 2.95 | 1.33 |
| 139 | Siliceous | Hydrogenetic | 1 | 0.11 | 2.05 | - | 0.05 | 0.06 | 0.05 | 0.12 |
|  |  |  | 2 | 0.18 | 1.00 | 0.00 | 0.02 | - | 0.18 | 0.02 |
|  |  |  | 3 | 0.32 | 1.97 | 0.01 | 0.03 | - | 0.16 | 0.04 |
|  |  |  | 4 | 0.47 | 1.17 | - | - | - | 0.40 | - |
|  |  |  | 5 | 0.10 | 2.03 | - | - | - | 0.05 | - |
|  |  |  | 6 | 16.86 | 19.63 | 0.25 | 0.11 | 0.35 | 0.86 | 0.71 |
|  |  |  | 7 | 21.10 | 18.34 | 0.29 | 0.26 | 0.19 | 1.15 | 0.73 |
|  |  |  | 8 | 18.99 | 15.64 | 0.28 | 0.21 | 0.46 | 1.21 | 0.95 |
|  |  |  | 9 | 8.07 | 8.65 | 0.12 | 0.12 | 0.08 | 0.93 | 0.33 |
|  |  |  | 10 | 15.84 | 20.04 | 0.23 | 0.11 | 0.34 | 0.79 | 0.68 |
|  |  |  | 11 | 22.22 | 15.40 | 0.19 | 0.44 | 0.67 | 1.44 | 1.30 |
|  |  |  | 12 | 1.52 | 1.27 | 0.02 | 0.01 | 0.07 | 1.19 | 0.11 |
|  |  |  | 13 | 2.34 | 6.56 | 0.02 | 0.04 | 0.13 | 0.36 | 0.19 |
|  |  |  | 14 | 17.90 | 18.45 | 0.27 | 0.08 | 0.06 | 0.97 | 0.40 |
|  |  |  | 15 | 20.12 | 20.92 | 0.24 | 0.21 | - | 0.96 | 0.45 |
|  |  |  | 16 | 18.88 | 20.56 | 0.29 | 0.15 | 0.37 | 0.92 | 0.81 |
|  |  |  | 17 | 21.11 | 19.49 | 0.25 | 0.15 | 0.06 | 1.08 | 0.46 |
|  |  |  | 18 | 17.25 | 19.71 | 0.22 | 0.02 | 0.33 | 0.88 | 0.57 |
|  |  |  | 19 | 22.47 | 18.90 | 0.15 | 0.10 | 0.21 | 1.19 | 0.45 |
|  |  |  | 20 | 19.23 | 21.30 | 0.13 | 0.16 | 0.63 | 0.90 | 0.93 |
|  |  |  | 21 | 13.10 | 11.05 | 0.06 | 0.21 | 0.53 | 1.19 | 0.79 |

| Sample | Host sediment | Genetic type | DataSet/Point | Mn | Fe | Co | Ni | Cu | Mn/Fe | Ni+Cu+Co |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 201F | Red clay | Mixed | 1 | 0.10 | 0.28 | 0.00 | 0.01 | 0.06 | 0.36 | 0.07 |
|  |  |  | 2 | 0.07 | 0.26 | 0.00 | 0.11 | 0.08 | 0.26 | 0.19 |
|  |  |  | 3 | 0.04 | 0.08 | - | 0.06 | 0.02 | 0.50 | 0.08 |
|  |  |  | 4 | 0.07 | 0.11 | 0.00 | 0.06 | 0.01 | 0.64 | 0.07 |
|  |  |  | 5 | 0.07 | 0.09 | - | - | 0.18 | 0.82 | 0.18 |
|  |  |  | 6 | 0.04 | 0.07 | - | - | - | 0.55 | - |
|  |  |  | 7 | 0.02 | 0.07 | - | 0.09 | - | 0.22 | 0.09 |
|  |  |  | 8 | 0.12 | 0.16 | 0.00 | 0.01 | 0.05 | 0.75 | 0.06 |
|  |  |  | 9 | 0.05 | 0.12 | - | 0.11 | 0.20 | 0.37 | 0.31 |
|  |  |  | 10 | 2.21 | 2.22 | 0.01 | 0.07 | 0.05 | 1.00 | 0.13 |
|  |  |  | 11 | 0.05 | 0.05 | - | - | 0.02 | 1.16 | 0.02 |
|  |  |  | 12 | 0.07 | 0.19 | - | 0.00 | 0.01 | 0.37 | 0.01 |
|  |  |  | 13 | 27.57 | 11.59 | 0.09 | 0.31 | 0.44 | 2.38 | 0.84 |
|  |  |  | 14 | 17.99 | 17.99 | 0.09 | 0.15 | 0.31 | 1.00 | 0.55 |
|  |  |  | 15 | 22.34 | 13.98 | 0.07 | 0.17 | 0.59 | 1.60 | 0.83 |
|  |  |  | 16 | 18.29 | 12.39 | 0.06 | 0.29 | 0.35 | 1.48 | 0.70 |
|  |  |  | 17 | 26.46 | 13.04 | 0.05 | 0.39 | 0.62 | 2.03 | 1.06 |
|  |  |  | 18 | 0.24 | 8.90 | - | 0.06 | 0.02 | 0.03 | 0.08 |
|  |  |  | 19 | 0.26 | 8.40 | 0.00 | - | 0.26 | 0.03 | 0.26 |
|  |  |  | 20 | 0.22 | 8.83 | 0.00 | - | 0.24 | 0.02 | 0.24 |
|  |  |  | 21 | 0.19 | 8.22 | 0.01 | 0.04 | 0.21 | 0.02 | 0.26 |
|  |  |  | 22 | 23.36 | 13.33 | 0.09 | 0.31 | 0.69 | 1.75 | 1.09 |
|  |  |  | 23 | 26.74 | 13.32 | 0.09 | 0.24 | 0.50 | 2.01 | 0.82 |
|  |  |  | 24 | 27.56 | 10.84 | 0.10 | 0.25 | 0.71 | 2.54 | 1.06 |
|  |  |  | 25 | 24.64 | 14.53 | 0.09 | 0.28 | 0.54 | 1.70 | 0.92 |
|  |  |  | 26 | 0.45 | 1.65 | - | 0.00 | - | 0.27 | 0.00 |
|  |  |  | 27 | 0.22 | 4.05 | - | 0.05 | 0.05 | 0.05 | 0.09 |
|  |  |  | 28 | 9.63 | 2.78 | 0.00 | 0.35 | 0.77 | 3.47 | 1.13 |
|  |  |  | 29 | 0.19 | 6.51 | - | 0.01 | 0.07 | 0.03 | 0.08 |
|  |  |  | 30 | 0.22 | 2.00 | - | 0.02 | 0.02 | 0.11 | 0.03 |