SUPPLEMENTARY INFORMATION

Scandium: An efficient dopant to modulate the optical spectrum of vanadium dioxide (VO2)

Devanshi Bhardwaj*, A. M. Umarji

Materials Research Centre, Indian Institute of Science, Bengaluru, India - 560012

*devanshib@iisc.ac.in

Figure S1: SEM images of (a) BV, (b) BVS1.0, (c) BVS2.0 and (d) BVS6.25 samples.

Figure S2:  V2p and O1s spectra for RTV and RTVS2.0 thin films.

Figure S3: Reflectance spectra (a) heating; (b) cooling for RTV thin film; Reflectance spectra (c) heating; (d) cooling for RTVS2.0 thin film

Table S1:  Raman modes of (a) V2O5 and (b) VO2 thin films compared with the literature.

| Modes | V2O5 | Modes | VO2 |
| --- | --- | --- | --- |
|  | Present Work | Ref.1 |  | Present Work | Ref.2 |
| Ag | 98.6 | 97 | B1g | 130 | 139 |
| B3g | 139 | 139 | Ag | 138 | 136 |
| Ag | 191 | 200 | Ag | 221 | 223 |
| B1g | 280 | 283 | Ag | 256 | 260 |
| B2g | 298.8 | 310 | Ag | 302 | 308 |
| Ag | 399.9 | 406 | Ag | 335 | 338 |
| Ag | 476.6 | 480 | Ag | 384 | 386 |
| Ag | 523.4 | 526 | Ag | 437 | 437 |
| B3g | 695.8 | 701 | Eg | - | 441 |
| Ag | 989 | 1000 | Ag | 493 | 500 |
|  |  |  | A1g | 611 | 616 |
|  |  |  | B2g | 813 | 825 |

Reference:

- Zhou, B.; He, D. Raman spectrum of vanadium pentoxide from density-functional perturbation theory. J. Raman Spectrosc. 2008, 39, 1475–1481.

- Wu, J. M.; Liou, L. B. Room temperature photo-induced phase transitions of VO2 nanodevices. J. Mater. Chem. 2011, 21, 5499–5504.